Tianjin dimethylaminoethyl methacrylate nanofiltration membrane development data set (2020-2021)

DOI：10.12072/ncdc.MDBW.db0008.2021

CSTR：11738.11.ncdc.MDBW.2021.6

Share type:Apply to Access

Category:Others

Datasets description

Data source description

Experimental data.

Data processing method

The membrane material PDM is self-made in the laboratory, and the PES ultrafiltration membrane (with a retained molecular weight of 50kDa) is purchased from zhongkerui Yang Membrane Technology Co., Ltd. The self-made nanofiltration membrane evaluation equipment in the laboratory is adopted. The membrane tank is made of stainless steel and the effective membrane area is 19.6 cm2. MgSO4 aqueous solution with a concentration of 1000 mg / l was prepared as the feed solution, the operating temperature was 25 ℃, preloaded at 0.9 MPa for 2 h, and the filtration test was carried out at 0.8 MPa.   Record the volume of permeate in a certain time, and calculate the membrane water flux according to formula (1): J = V / (s) × t) (1) where, J represents water flux, unit: L / (m2h); V is the volume of permeate, in L; S is the effective filtration area of the membrane, in m2; T is the water flux test time, in H. The rejection rate of inorganic salt is calculated according to formula (2): r = (c_f-c_p) / C_ f × 100 (2), where R is the salt rejection rate, in%, CF is the feed liquid conductivity, and CP is the permeate liquid conductivity.

Data quality description

(1) Data production process: the self-made composite membrane was used to measure the permeate volume and conductivity by nanofiltration evaluation device, and the flux and salt rejection were calculated.   (2) Methods and standard specifications: three parallel experiments were conducted under each experimental condition.  (3) Results: PDM nanofiltration membrane could be prepared quickly and had good desalination performance.

Base information

collect time:2020/01/01-2021/09/30

collect place:Tianjin

data size:81.6 KiB

data format:excel

Coordinate system: 无

Keywords

Theme:Quaternary amination, nanofiltration membrane
	Subject:Fundamentals of Engineering and Technical Sciences 
	Time:2020 2021
	Place:Tianjin

Space scope

|  | north： |  |
| --- | --- | --- |
| west： |  | east： |
|  | south： |  |

Service information

contacts:Min Yufang

phone:0931-4967596

mailbox:ncdc@lzb.ac.cn

Contact information

contributors:DU Runhong

author:DU Runhong

manager:DU Runhong

Project information

number:2017YFE0114200，
      name:

Citations and annotations

In order to protect the rights and interests of the platform's scientific and technological resources, expand the services of the platform center, and enhance the application potential of scientific and technological resources,resource users are requested to mark and quote the research results (including published papers, treatises, data products, unpublished research reports, data products, etc.) generated by the use of resources in the following manner.

For the achievements published in English, please refer to the following specifications：

The dataset is provided by National Cryosphere Desert Data Center(https://www.ncdc.ac.cn).

Data reference:

DU Runhong. Tianjin dimethylaminoethyl methacrylate nanofiltration membrane development data set (2020-2021). National Cryosphere Desert Data Center(http://www.ncdc.ac.cn), 2021. https://cstr.cn/CSTR:11738.11.ncdc.MDBW.2021.6.