Test data set of non-metallic materials of drilling tools (2017-2018)

DOI：10.12072/ncdc.SRIPE.db1696.2022

CSTR：11738.11.ncdc.SRIPE.db1696.2022

Share type:Apply to Access

Category:Others

Datasets description

From 2017 to 2018, 8 pieces of test data of mechanical properties of rubber materials were obtained by indoor test method in Wuhan, Hubei Province, including tensile properties, compressive properties, bending properties, peeling properties, etc. After low temperature storage at - 50 ℃, the material was taken out for performance test. The test results show that the material meets the requirements of low temperature storage at - 50 ℃. The data set includes Mooney viscosity at 100 ℃, results, vulcanization curve, time for torque to reach 10% of maximum value, time for torque to reach 90% of maximum value, minimum torque value, maximum torque value, tensile strength, elongation at break, 50% elongation at break, 100% elongation at break, tear strength, permanent set at break, hardness, first peak load, maximum point load, 90 ° Peel strength and fracture condition。

Data source description

The data set includes Mooney viscosity at 100 ℃, results, vulcanization curve, time for torque to reach 10% of maximum value, time for torque to reach 90% of maximum value, minimum torque value, maximum torque value, tensile strength, elongation at break, 50% elongation at break, 100% elongation at break, tear strength, permanent set at break, hardness, first peak load, maximum point load, 90 ° Peel strength and fracture condition.

Data processing method

The instruments used for data acquisition include gt-m2000a rotor less rheometer, smv-300rt Mooney viscometer and ags-j electronic tensile testing machine. The test methods refer to GB / T 528-2009, GB / T 529-2008 and GB / T 531.1-2008</ p>

Data quality description

Good data quality

Base information

collect time:2017/01/01-2018/12/30

collect place:Hubei Wuhan Sinopec jiangzhan Petroleum Machinery Co., Ltd

data size:10.8 MiB

data format:

Coordinate system: 无

Keywords

Theme:Rubber, tensile strength, tear strength
	Subject:geology 
	Time:2017 2018
	Place:Wuhan City

Space scope

|  | north： |  |
| --- | --- | --- |
| west： |  | east： |
|  | south： |  |

Service information

contacts:Min Yufang

phone:0931-4967596

mailbox:ncdc@lzb.ac.cn

Contact information

contributors:chi shenggao

author:Wu gang

manager:Wu gang

Project information

number:2016YFC0303300，
      name:

Citations and annotations

In order to protect the rights and interests of the platform's scientific and technological resources, expand the services of the platform center, and enhance the application potential of scientific and technological resources,resource users are requested to mark and quote the research results (including published papers, treatises, data products, unpublished research reports, data products, etc.) generated by the use of resources in the following manner.

For the achievements published in English, please refer to the following specifications：

The dataset is provided by National Cryosphere Desert Data Center(https://www.ncdc.ac.cn).

Data reference:

chi shenggao. Test data set of non-metallic materials of drilling tools (2017-2018). National Cryosphere Desert Data Center(http://www.ncdc.ac.cn), 2022. https://cstr.cn/CSTR:11738.11.ncdc.SRIPE.db1696.2022.