Test data set of water blocking layer modification and reconstruction technology in alpine Kuangqu mining area (2022-2025)

Share type:Login to Access

Category:Others

Datasets description

Data source description

Indoor soil column infiltration test: Different coal gangue particle sizes (2-5 mm, 0.5~2 mm,

Data processing method

(1) Use SPSS25.0 statistical software to conduct correlation factor analysis;   (2) Use Origin 2021 software to fit the Green-Ampt mechanism model, Philip model, and Kostiakov empirical model, and calculate the root mean square error (RMSE), mean absolute error (MAE), coincidence index (D) and coefficient of determination (R2);  (3) The experimental data were systematically organized using Microsoft Excel software.

Data quality description

Three standard indicators: root-mean-square error (RMSE), mean absolute error (MAE), coincidence index (D) and coefficient of determination (R2) were used to verify the errors between Philip's model, Kostiakov's empirical model and actual data. The water blocking effects of different water blocking layers are verified by using infiltration rate, cumulative infiltration volume, and water blocking effect. The results show that the gradation of coal gangue crushed matter is 2:5:3(1~2mm, 0.5~1mm,<0.5 mm), the bulk weight of coal gangue crushed matter is controlled to be 1.60~ 1.75 g/cm2, the W-OH concentration is 3.5~4.5%, the spraying amount is 2.5~ 3.5 L/m2, and the PAM sowing amount is dry sprinkled on the surface of the compacted coal gangue in the range of 0.05~ 0.07 g/cm2, the best effect of resisting water is achieved.

Base information

collect time:2022/09/01-2025/06/11

collect place:China, Qinghai Tibet Muli Mining Area

data size:21.8 MiB

data format:*.xlsx

Coordinate system: 无

Keywords

Theme:coal gangue, Infiltration rate, Aquiclude
	Subject:Geography and other disciplines 
	Time:2022 2023 2024 2025
	Place:China,  Muli Kuangqu

Space scope

|  | north： 38.14 |  |
| --- | --- | --- |
| west： 99.13 |  | east： 99.12 |
|  | south： 38.12 |  |

Service information

contacts:None

phone:13911040827.0

mailbox:yang_hlong@163.com

Contact information

contributors:yang hai long,  lu chang jin,  yin wen tian,  wu miao chen

author:yang hai long ,  lu chang jin ,  yin wen tian ,  wu miao chen

manager:yang hai long , lu chang jin , yin wen tian , wu miao chen

Project information

number:2022YFF1302604，
      name:

Citations and annotations

In order to protect the rights and interests of the platform's scientific and technological resources, expand the services of the platform center, and enhance the application potential of scientific and technological resources,resource users are requested to mark and quote the research results (including published papers, treatises, data products, unpublished research reports, data products, etc.) generated by the use of resources in the following manner.

For the achievements published in English, please refer to the following specifications：

The dataset is provided by National Cryosphere Desert Data Center(https://www.ncdc.ac.cn).

Data reference:

yang hai long, lu chang jin, yin wen tian, wu miao chen. Test data set of water blocking layer modification and reconstruction technology in alpine Kuangqu mining area (2022-2025). National Cryosphere Desert Data Center(http://www.ncdc.ac.cn), 2026.