Overall Desalination Rate Dataset for Tianjin Jinhai Lake Water Desalination System (July-September 2020)

DOI：10.12072/ncdc.MDBW.db0015.2021

CSTR：11738.11.ncdc.MDBW.2021.18

Share type:Login to Access

Category:Others

Datasets description

Jinhai Lake water is desalinated by reverse osmosis/nanofiltration system after precision filtration-ultrafiltration pretreatment. The desalination rate of the desalination system was examined under different mixing methods and different operating pressures. The desalination system used commercial polyamide 4040 rolled nanofiltration and reverse osmosis membrane modules (VNF2 and ULP100, Guiyang Times Walton Co., Ltd.). After the pressure and flow rate were stabilized for half an hour, the salt content of the produced water from the desalination system was recorded and calculated to obtain the overall desalination rate. The operating pressure was 1.3-1.8MPa, the salt content of the influent water was 7.5g/L, the water temperature was 30±2℃, the influent water flow rate was 2m3/h, and the number of membrane modules was 6-8. The measurement is accurate to two decimal places. The overall desalination rate of the desalination system is more than 90%, reaching the assessment index of the task book. This dataset is mainly applied to the study of brackish water desalination.

Data source description

Experimentally obtained.

Data processing method

Operating pressure 1.3~1.8 MPa, inlet water salinity 7.5 g/L, water temperature 30 ± 2 ℃, inlet water flow rate 2 m3/h when the experimental measurements of the salinity of the produced water, the calculation of the desalination rate obtained.

Data quality description

(1) Data production process: after the lake water of Jinhai Lake was pre-treated by precision filtration-ultrafiltration, the pre-treated effluent was pumped by a high-pressure pump (CRN3-29, Grundfos) into the reverse osmosis/nano-filtration desalination system, and the desalination system used the commercial polyamide 4040 rolled-type nano-filtration and reverse osmosis membrane modules (VNF2 and ULP100, Guiyang Times Walden Co., Ltd.). After the pressure and flow rate were stabilized for half an hour, the salt content of the produced water from the desalination system was recorded and calculated to obtain the overall desalination rate.   (2) Methods: operating pressure 1.3-1.8 MPa, influent salinity 7.5 g/L, water temperature 30 ± 2°C, influent flow rate 2 m3/h, and the number of membrane modules is 6-8 pieces. The measurement is accurate to two decimal places.   (3) Result: the overall desalination rate of the desalination system is more than 90%, reaching the assessment index of the task book.

Base information

collect time:2020/07/20-2020/09/30

collect place:Jinhai Lake, Binhai New Area, Tianjin

data size:110.1 KiB

data format:excel

Coordinate system: 无

Keywords

Theme:Nanofiltration, reverse osmosis, pretreatment, mixed loading, desalination rate
	Subject:Hydrochemistry 
	Time:2020
	Place:Jinhai Lake

Space scope

|  | north： |  |
| --- | --- | --- |
| west： |  | east： |
|  | south： |  |

Service information

contacts:Min Yufang

phone:0931-4967596

mailbox:ncdc@lzb.ac.cn

Contact information

contributors:DU Runhong

author:DU Runhong

manager:DU Runhong

Project information

number:2017YFE0114200，
      name:

Citations and annotations

In order to protect the rights and interests of the platform's scientific and technological resources, expand the services of the platform center, and enhance the application potential of scientific and technological resources,resource users are requested to mark and quote the research results (including published papers, treatises, data products, unpublished research reports, data products, etc.) generated by the use of resources in the following manner.

For the achievements published in English, please refer to the following specifications：

The dataset is provided by National Cryosphere Desert Data Center(https://www.ncdc.ac.cn).

Data reference:

DU Runhong. Overall Desalination Rate Dataset for Tianjin Jinhai Lake Water Desalination System (July-September 2020). National Cryosphere Desert Data Center(http://www.ncdc.ac.cn), 2021. https://cstr.cn/CSTR:11738.11.ncdc.MDBW.2021.18.