Dataset on the Template Effect of Crosslinking Agents on Anionic Imprinted Polymers (September 2018)

DOI：10.12072/ncdc.UTCMW.db2131.2022

CSTR：11738.11.ncdc.UTCMW.db2131.2022

Share type:Login to Access

Category:Others

Datasets description

The template effect is considered the most important feature of ion imprinted polymer (IIP) technology. However, there is still a certain gap in the theoretical and practical application of template effects. In this study, we propose a method to control the template effect of IIPs by adjusting the crosslinking ratio. A series of Cr (VI) - IIPs with different crosslinking agent contents were synthesized. On the basis of qualitative analysis of coordination selectivity and template effect, a theoretical equation for the template effect generated by crosslinking agents was established using the Scatchard equation. In the Cr (VI) removal process, when the molar ratio of functional monomer to crosslinking agent is 1/5.46, the contribution of template effect begins to exceed that of coordination effect, and with the increase of crosslinking agent content, the template effect is further enhanced. In practical wastewater treatment applications, IIP-1/12 and IIP-1/6 designed based on the obtained equation can effectively treat two different types of wastewater. The standardized equation and design concept proposed in this study theoretically demonstrate the effect of crosslinking agents on material selectivity. This provides greater flexibility for the design and application of template effects in ion imprinting technology. The effect of crosslinking agents on the template effect of polymers: Taking anionic imprinted polymers as an example dataset, experimental methods were used to obtain data in decimal (. xls) format, with a data volume of 13 groups and a total of 720 experimental data.

Data source description

Indoor experiments, formula reasoning, independently generated.

Data processing method

Use the Scatchard model coefficient system software module for modeling. The experiment used Cr (VI) - IIP and NIP with functional monomers/crosslinkers in molar ratios of 1/4, 1/6, 1/8, 1/10, 1/12, and 1/15 to perform adsorption experiments on different ion solutions such as 0.2, 2, and 6 mmol/L, and obtained data.

Data quality description

The data quality is good.

Base information

collect time:2018/09/01-2018/09/30

collect place:Nanchang City, Jiangxi Province

data size:809.2 KiB

data format:Excel

Coordinate system: 无

Keywords

Theme:Crosslinking agent, template effect, ion imprinted polymer
	Subject:geology 
	Time:2018
	Place:Nanchang City

Space scope

|  | north： 29.17 |  |
| --- | --- | --- |
| west：116.55 |  | east：115.45 |
|  | south： 28.12 |  |

Service information

contacts:Min Yufang

phone:0931-4967596

mailbox:ncdc@lzb.ac.cn

Contact information

contributors:Yang Liming

author:Yang Liming

manager:MIN Yufang

Project information

number:2018YFC0406400，
      name:

Citations and annotations

In order to protect the rights and interests of the platform's scientific and technological resources, expand the services of the platform center, and enhance the application potential of scientific and technological resources,resource users are requested to mark and quote the research results (including published papers, treatises, data products, unpublished research reports, data products, etc.) generated by the use of resources in the following manner.

For the achievements published in English, please refer to the following specifications：

The dataset is provided by National Cryosphere Desert Data Center(https://www.ncdc.ac.cn).

Data reference:

Yang Liming. Dataset on the Template Effect of Crosslinking Agents on Anionic Imprinted Polymers (September 2018). National Cryosphere Desert Data Center(http://www.ncdc.ac.cn), 2022. https://cstr.cn/CSTR:11738.11.ncdc.UTCMW.db2131.2022.