Tianjin Jinhai Lake Water Nanofiltration Hardness Removal Rate Dataset (July-September 2020)

DOI：10.12072/ncdc.MDBW.db0020.2021

CSTR：11738.11.ncdc.MDBW.2021.15

Share type:Login to Access

Category:Others

Datasets description

After the lake water of Jinhai Lake was pre-treated by precision filtration-ultrafiltration, the pre-treated effluent was pumped by a high-pressure pump (CRN3-29, Grundfos) into the desalination system equipped with different numbers of nanofiltration membranes, which were made of commercialized polyamide 4040 rolled-type membrane modules (VNF2, Guiyang Times Walden Co., Ltd.). After the pressure and flow rate were stabilized for half an hour, water samples of produced water were collected, and the calcium and magnesium ion content was determined by a third-party testing organization to calculate the calcium and magnesium removal rate. The operating pressure was 1.3 MPa, the salt content of the influent water was 7.5 g/L, the water temperature was 30 ± 2°C, the influent flow rate was 2 m3/h, and the number of membrane modules was 6-8 pieces. Calcium and magnesium ion content determination according to the “standard test methods for drinking water” GB/T 15452-2009 standard specification of the test method and process. Measurement is accurate to two decimal places. The removal rate of calcium and magnesium ions by nanofiltration desalination system is greater than 98.45% and 98.72% respectively, which reaches the assessment index of the task book.

Data source description

Experimentally obtained.

Data processing method

Operating pressure of 1.3 MPa, inlet water salinity of 7.5 g/L, water temperature of 30 ± 2 ℃, inlet water flow rate of 2 m3/h under the conditions of collection of nanofiltration desalination water. The calcium and magnesium ion content of the lake water and nanofiltration produced water was measured by a third-party testing organization.

Data quality description

(1) Data production process: after the lake water of Jinhai Lake is pre-treated by precision filtration-ultrafiltration, the pre-treated effluent is pumped by a high-pressure pump (CRN3-29, Grundfos) into the desalination system equipped with different quantities of nano-filtration membranes, which are made of commercialized polyamide 4040 rolled membrane module (VNF2, Guiyang Times Walden Co., Ltd.). After the pressure and flow rate were stabilized for half an hour, water samples of produced water were collected, and the calcium and magnesium ion content was determined by a third-party testing organization to calculate the calcium and magnesium removal rate.   (2) Methods: operating pressure 1.3 MPa, influent salt content 7.5 g/L, water temperature 30 ± 2 ℃, influent flow rate 2 m3/h, the number of membrane modules for 6-8. Calcium and magnesium ion content determination according to the “standard test methods for drinking water” GB/T 15452-2009 standard specification test methods and processes. The measurement is accurate to two decimal places.   (3) Results: the removal rate of calcium and magnesium ions by the nanofiltration desalination system is greater than 98.45% and 98.72%, respectively, and reaches the assessment index of the task book.

Base information

collect time:2020/07/20-2020/09/20

collect place:Jinhai Lake, Binhai New Area, Tianjin

data size:530.0 KiB

data format:excel

Coordinate system: 无

Keywords

Theme:Nanofiltration, calcium ion, magnesium ion
	Subject:Hydrochemistry 
	Time:2020
	Place:Jinhai Lake

Space scope

|  | north： |  |
| --- | --- | --- |
| west： |  | east： |
|  | south： |  |

Service information

contacts:Min Yufang

phone:0931-4967596

mailbox:ncdc@lzb.ac.cn

Contact information

contributors:DU Runhong

author:DU Runhong

manager:DU Runhong

Project information

number:2017YFE0114200，
      name:

Citations and annotations

In order to protect the rights and interests of the platform's scientific and technological resources, expand the services of the platform center, and enhance the application potential of scientific and technological resources,resource users are requested to mark and quote the research results (including published papers, treatises, data products, unpublished research reports, data products, etc.) generated by the use of resources in the following manner.

For the achievements published in English, please refer to the following specifications：

The dataset is provided by National Cryosphere Desert Data Center(https://www.ncdc.ac.cn).

Data reference:

DU Runhong. Tianjin Jinhai Lake Water Nanofiltration Hardness Removal Rate Dataset (July-September 2020). National Cryosphere Desert Data Center(http://www.ncdc.ac.cn), 2021. https://cstr.cn/CSTR:11738.11.ncdc.MDBW.2021.15.