Test data set of relationship between elastic modulus and erosion depth

DOI：10.12072/ncdc.nieer.db2788.2023

CSTR：11738.11.NCDC.NIEER.DB2788.2023

Share type:Apply to Access

Category:Others

Datasets description

<pre><code> &lt;p&gt;&amp;emsp;&amp;emsp; In order to simulate the corrosion damage and deterioration rule of concrete in seawater environment, indoor corrosion tests were carried out on concrete samples with 10% Na&lt;sub&gt;2&lt;/sub&gt;SO&lt;sub&gt;4&lt;/sub&gt;solution under different osmotic pressures and different time lengths. Combined with the micro indentation test, CT scanning test and electron microscope scanning test, the corrosion damage and micromechanical properties of concrete under the high permeability sulfate coupling corrosion were studied. The test results showed that: (1) The osmotic pressure accelerated the ion migration, mainly played a role in promoting chemical corrosion. (2) The greater the osmotic pressure is, the faster the chemical damage rate of concrete is, and the deeper the erosion depth is. (3) The bond between aggregate and mortar is a weak point that is easy to erode and damage (4) The internal pores of concrete are easy to generate hydration products, and a large number of short column gypsum crystals and fine needle ettringite crystals are easy to be generated under high osmotic pressure.

Data source description

<pre><code> &lt;p&gt;&amp;emsp;&amp;emsp; The data comes from the test measurement.

Data processing method

<pre><code> &lt;p&gt;&amp;emsp;&amp;emsp; Combined with micro indentation test, CT scanning test and electron microscope scanning test, the corrosion damage and micromechanical properties of concrete under high permeability sulfate coupling corrosion were studied.

Data quality description

<pre><code> &lt;p&gt;&amp;emsp;&amp;emsp; The data quality is good.

Base information

collect time:2021/03/01-2021/03/31

collect place:Wuhan, Hubei

data size:25.7 KiB

data format:

Coordinate system: 无

Keywords

Theme:High permeability, sulfate attack, concrete, micron indentation, micromechanics
	Subject:Geography and other disciplines 
	Time:2021
	Place:Wuhan

Space scope

|  | north： |  |
| --- | --- | --- |
| west： |  | east： |
|  | south： |  |

Service information

contacts:Minyufang

phone:0931-4967596

mailbox:ncdc@lzb.ac.cn

Contact information

contributors:LI Ruixin

author:LI Ruixin

manager:LI Ruixin

Project information

number:2018YFC0809600，
      name:

Citations and annotations

In order to protect the rights and interests of the platform's scientific and technological resources, expand the services of the platform center, and enhance the application potential of scientific and technological resources,resource users are requested to mark and quote the research results (including published papers, treatises, data products, unpublished research reports, data products, etc.) generated by the use of resources in the following manner.

For the achievements published in English, please refer to the following specifications：

The dataset is provided by National Cryosphere Desert Data Center(https://www.ncdc.ac.cn).

Data reference:

LI Ruixin. Test data set of relationship between elastic modulus and erosion depth. National Cryosphere Desert Data Center(http://www.ncdc.ac.cn), 2023. https://cstr.cn/CSTR:11738.11.NCDC.NIEER.DB2788.2023.