Dataset of anti-interference ability of rich defect porous carbon through remote hydrophobic synergistic dispersion adsorption of bisphenol A (August 2018 November 2019)

DOI：10.12072/ncdc.UTCMW.db2162.2022

CSTR：11738.11.ncdc.UTCMW.db2162.2022

Share type:Login to Access

Category:Others

Datasets description

The wastewater characteristic oriented design adsorbent is a promising but challenging strategy for sustainable remediation of actual bisphenol A (BPA) pollution. Research has shown that waste cigarette butt activated carbon (AC-800) has high capacity (865 mg/g), rapid reaction rate (186.9 mg/g/min), and excellent BPA adsorption durability. Unlike carbon based adsorbents reported in literature, quantitative structure-activity relationship studies reveal that graphite defects play a crucial role in improving the adsorption performance of adsorbents. Further research has shown that π - π interactions, electrostatic attraction, and hydrogen bonding interactions have negligible effects on AC-800, while long-range hydrophobic interactions and short-range dispersion forces contribute significantly to BPA adsorption. Thanks to its unique adsorption mechanism, AC-800 has significant anti-interference ability, achieving efficient purification of BPA in complex background wastewater. This study provides new insights into the adsorption mechanism of bisphenol A on carbon based materials and develops an adsorbent suitable for practical green wastewater remediation. Rich defect porous carbon adsorbs bisphenol A through remote hydrophobic interaction and short-range dispersion force, with anti-interference ability dataset obtained by experimental methods. The data format is decimal (. xls), with 6 sets of data and a total of 41213 entries.

Data source description

Indoor experiments, instrument characterization, independently generated.

Data processing method

Characterization using BET, XRD, XPS, Raman spectroscopy SEM、 Characterize system software modules such as elemental analysis data processing.

Data quality description

The data quality is good.

Base information

collect time:2018/08/09-2019/11/08

collect place:Nanchang City, Jiangxi Province

data size:7.6 MiB

data format:Excel

Coordinate system: 无

Keywords

Theme:Remote hydrophobic interaction, BPA adsorption, carbon based materials
	Subject:geology 
	Time:2018 2019
	Place:Nanchang City

Space scope

|  | north： 29.17 |  |
| --- | --- | --- |
| west：116.55 |  | east：115.45 |
|  | south： 28.12 |  |

Service information

contacts:Min Yufang

phone:0931-4967596

mailbox:ncdc@lzb.ac.cn

Contact information

contributors:Yang Liming

author:Yang Liming

manager:MIN Yufang

Project information

number:2018YFC0406400，
      name:

Citations and annotations

In order to protect the rights and interests of the platform's scientific and technological resources, expand the services of the platform center, and enhance the application potential of scientific and technological resources,resource users are requested to mark and quote the research results (including published papers, treatises, data products, unpublished research reports, data products, etc.) generated by the use of resources in the following manner.

For the achievements published in English, please refer to the following specifications：

The dataset is provided by National Cryosphere Desert Data Center(https://www.ncdc.ac.cn).

Data reference:

Yang Liming. Dataset of anti-interference ability of rich defect porous carbon through remote hydrophobic synergistic dispersion adsorption of bisphenol A (August 2018 November 2019). National Cryosphere Desert Data Center(http://www.ncdc.ac.cn), 2022. https://cstr.cn/CSTR:11738.11.ncdc.UTCMW.db2162.2022.