A novel collector dataset with wide pH adaptability and high selectivity for flotation separation of scheelite and calcite (March 2020)

DOI：10.12072/ncdc.UTCMW.db2190.2022

CSTR：11738.11.ncdc.UTCMW.db2190.2022

Share type:Login to Access

Category:Others

Datasets description

Efficient separation of gangue minerals in scheelite flotation is a persistent scientific research topic. Due to the further scarcity and impurities of scheelite resources, as well as limited industrial production input costs, flotation reagents must meet the requirements in terms of source, price, and efficiency. Cationic collectors are a promising flotation agent for scheelite at room temperature, such as quaternary ammonium salt cationic collectors, which have shown good flotation performance in silicate flotation processes. Compared with quaternary ammonium salts, quaternary ammonium salts are almost unaffected by pH changes and have good pH applicability. Therefore, quaternary ammonium salt groups are an ideal choice for constructing novel collectors that can adapt to a wider pH range. Compared with traditional surfactants, Gemini surfactants have higher activity and can also utilize Gemini's quaternary ammonium structure to build collector affinity groups, enhancing the adsorption response of scheelite surface. As mentioned above, gemini surfactant may be an ideal collector for scheelite foam flotation. More importantly, Gemini surfactants have never been reported for the flotation of scheelite. This article mainly studies the flotation laws and mechanisms of new collectors on calcium containing minerals, which is of great significance for the room temperature flotation of scheelite. The results showed that the flotation behavior of Gemini cationic collector HDDA on scheelite and its vein mineral calcite single mineral was studied. At pH 6-11 and a concentration of 0.5 × 10-4mol/L collector, the new Gemini quaternary ammonium salt collector showed excellent selectivity in the separation of scheelite and calcite experiments. Compared with NaOH, HDDA exhibited superior flotation performance. Supported by the experimental conclusions of single mineral experiments, flotation separation of artificially mixed minerals was carried out using 0.5 × 10-4mol/L HDDA and NaOL as collectors under different pH conditions. Based on the data of yield and recovery rate, it can be further proved that HDDA is a collector with excellent selectivity for scheelite and calcite. During the flotation experiment, various datasets were obtained through experimental methods and formula inference calculations. The data format was decimal (. xls), with a total of 16 experiments and 3 sets of data.

Data source description

Indoor experiment, independently generated.

Data processing method

During the flotation experiment, various datasets were obtained through experimental methods and formula inference calculations.

Data quality description

The data quality is good.

Base information

collect time:2020/03/01-2020/03/31

collect place:Nanchang City, Jiangxi Province

data size:491.6 KiB

data format:Excel

Coordinate system: 无

Keywords

Theme:Scheelite, calcite, flotation separation
	Subject:geology 
	Time:2020
	Place:Nanchang City

Space scope

|  | north： 29.17 |  |
| --- | --- | --- |
| west：116.55 |  | east：115.45 |
|  | south： 28.12 |  |

Service information

contacts:Min Yufang

phone:0931-4967596

mailbox:ncdc@lzb.ac.cn

Contact information

contributors:Yang Liming

author:Yang Liming

manager:MIN Yufang

Project information

number:2018YFC0406400，
      name:

Citations and annotations

In order to protect the rights and interests of the platform's scientific and technological resources, expand the services of the platform center, and enhance the application potential of scientific and technological resources,resource users are requested to mark and quote the research results (including published papers, treatises, data products, unpublished research reports, data products, etc.) generated by the use of resources in the following manner.

For the achievements published in English, please refer to the following specifications：

The dataset is provided by National Cryosphere Desert Data Center(https://www.ncdc.ac.cn).

Data reference:

Yang Liming. A novel collector dataset with wide pH adaptability and high selectivity for flotation separation of scheelite and calcite (March 2020). National Cryosphere Desert Data Center(http://www.ncdc.ac.cn), 2022. https://cstr.cn/CSTR:11738.11.ncdc.UTCMW.db2190.2022.