Experimental dataset of RNRR deep processing unit for highly mineralized mine water in Dahaize, Yulin City, Shaanxi Province (March April 2021)

DOI：10.12072/ncdc.UTCMW.db2122.2022

CSTR：11738.11.ncdc.UTCMW.db2122.2022

Share type:Login to Access

Category:Others

Datasets description

RNRR multi-stage enhanced membrane concentration is based on the high desalination rate of RO membrane and the strong tolerance of NF membrane to organic and inorganic pollution. By combining the advantages of RO membrane and NF membrane, they complement each other, resulting in a concentrated water multi-stage enhanced membrane concentration treatment equipment with long cleaning cycle and service life, low operating cost, and high water production rate. Adopting RNRR multi-stage enhanced membrane concentration process for deep treatment of high salinity mine water, desalination treatment and reuse. The RNRR membrane concentration device consists of 18 reverse osmosis membranes and 6 nanofiltration membranes, including four sections. The 1 # RO section has 6 membranes in parallel, the 2 # NF section has 5 membranes in parallel, the 3 # RO section has 6 membranes in parallel, and the 4 # RO section has 6 membranes in parallel. The recovery rate of each section is adjustable from 60% to 85%, and it is adjusted according to the TDS mass concentration. After pretreatment, the raw water enters the intermediate water tank and then enters the membrane desalination system. Through experiments, the removal of various salt ions in highly mineralized mine water by RNRR multi-stage enhanced membrane concentration process under different operating parameters such as operating pressure, feed liquid temperature, and feed liquid concentration was obtained, as well as its effects on the membrane flux and membrane fouling changes of nanofiltration and reverse osmosis membranes. And obtained experimental data on optimizing control of each section to achieve an overall water recovery rate of over 85% in the process. In addition, experimental data on the cleaning of contaminated membranes were also obtained. The dataset contains a total of 17 sets of data, with each set containing 10-55 data points, and the dataset is fully open for sharing.

Data source description

R was obtained through indoor experimental methods, using simulated high salinity mine water artificially prepared from tap water as the raw water.

Data processing method

Using laboratory equipment and manually preparing simulated high salinity mine water for experiments, with a treatment scale of 0.5-1 m3/h, collect and process water samples for indicator testing.

Data quality description

Good data quality

Base information

collect time:2021/03/01-2021/04/30

collect place:Yulin City, Shaanxi Province

data size:2.4 MiB

data format:Excel

Coordinate system: 无

Keywords

Theme:High desalination rate, operating pressure, rnrr multistage enhanced membrane concentration, high salinity
	Subject:geology 
	Time:2021
	Place:Yulin

Space scope

|  | north： 38.97 |  |
| --- | --- | --- |
| west：110.40 |  | east：108.97 |
|  | south： 37.82 |  |

Service information

contacts:Min Yufang

phone:0931-4967596

mailbox:ncdc@lzb.ac.cn

Contact information

contributors:ZHENG Xi

author:ZHENG Xi

manager:MIN Yufang

Project information

number:2018YFC0406403，
      name:

Citations and annotations

In order to protect the rights and interests of the platform's scientific and technological resources, expand the services of the platform center, and enhance the application potential of scientific and technological resources,resource users are requested to mark and quote the research results (including published papers, treatises, data products, unpublished research reports, data products, etc.) generated by the use of resources in the following manner.

For the achievements published in English, please refer to the following specifications：

The dataset is provided by National Cryosphere Desert Data Center(https://www.ncdc.ac.cn).

Data reference:

ZHENG Xi. Experimental dataset of RNRR deep processing unit for highly mineralized mine water in Dahaize, Yulin City, Shaanxi Province (March April 2021). National Cryosphere Desert Data Center(http://www.ncdc.ac.cn), 2022. https://cstr.cn/CSTR:11738.11.ncdc.UTCMW.db2122.2022.