Data set of gas permeability change under different confining pressures

DOI：10.12072/ncdc.nieer.db2808.2023

CSTR：11738.11.NCDC.NIEER.DB2808.2023

Share type:Apply to Access

Category:Others

Datasets description

<pre><code> &lt;p&gt;&amp;emsp;&amp;emsp; The lining structure is subject to the three-dimensional stress transmitted by the overlying soil and rock stratum, and is usually subject to external sulfate erosion; The permeability and mechanical properties of cement materials are of great significance to the stability of underground works. The experimental results can provide reference materials for establishing the long-term stability of concrete structures in high sulfate environment. The data set adopts the geotechnical test method to analyze the changes of permeability, ultrasonic P-wave velocity, uniaxial compression and splitting tensile strength of sulfate eroded cement mortar specimens. (1) With the increase of the confining pressure, the gas permeability decreases gradually, and the gas permeability and decreasing amplitude of the corroded sample and the non corroded sample are different. (2) The gas permeability of the attacked specimen is large, and it is more sensitive to the change of confining pressure in the range of 5~20MPa; Under the high confining pressure of 20~30MPa, the decreasing rate of gas permeability decreases. (3) The ultrasonic P-wave velocity of the attacked sample is obviously lower than that of the non attacked sample, while its open porosity is higher than its corresponding sample. (4) The splitting tensile strength and uniaxial compressive strength decreased after sulfate attack, and the former deteriorated more seriously.

Data source description

<pre><code> &lt;p&gt;&amp;emsp;&amp;emsp; The data comes from the test measurement.

Data processing method

<pre><code> &lt;p&gt;&amp;emsp;&amp;emsp; The variation of permeability, ultrasonic P-wave velocity, uniaxial compression and splitting tensile strength of sulfate eroded cement mortar specimens were analyzed by geotechnical test method.

Data quality description

<pre><code> &lt;p&gt;&amp;emsp;&amp;emsp; The data quality is good.

Base information

collect time:2019/12/01-2019/12/31

collect place:Wuhan, Hubei

data size:26.6 KiB

data format:

Coordinate system: 无

Keywords

Theme:Degradation, leakage, strength and material testing of geotechnical materials
	Subject:geology 
	Time:2019
	Place:Wuhan

Space scope

|  | north： |  |
| --- | --- | --- |
| west： |  | east： |
|  | south： |  |

Service information

contacts:Minyufang

phone:0931-4967596

mailbox:ncdc@lzb.ac.cn

Contact information

contributors:HU Dawei

author:HU Dawei

manager:HU Dawei

Project information

number:2018YFC0809600，
      name:

Citations and annotations

In order to protect the rights and interests of the platform's scientific and technological resources, expand the services of the platform center, and enhance the application potential of scientific and technological resources,resource users are requested to mark and quote the research results (including published papers, treatises, data products, unpublished research reports, data products, etc.) generated by the use of resources in the following manner.

For the achievements published in English, please refer to the following specifications：

The dataset is provided by National Cryosphere Desert Data Center(https://www.ncdc.ac.cn).

Data reference:

HU Dawei. Data set of gas permeability change under different confining pressures. National Cryosphere Desert Data Center(http://www.ncdc.ac.cn), 2023. https://cstr.cn/CSTR:11738.11.NCDC.NIEER.DB2808.2023.