Research data set on mineral processing wastewater treatment of tungsten molybdenum ore containing salt hydroxamic acid (October 2018)

DOI：10.12072/ncdc.UTCMW.db2148.2022

CSTR：11738.11.ncdc.UTCMW.db2148.2022

Share type:Apply to Access

Category:Others

Datasets description

Taking the simulated flotation wastewater as the research object, the ozone oxidation method is used to treat it, and the value of CODcr is reduced to meet the class I discharge standard of integrated wastewater discharge standard (GB 8978-1996) and the quality of industrial water for urban wastewater recycling (GB/t 19923-2005). The experimental factors to be explored include reaction time, initial pH, ozone dosage, etc. The data set contains 245 data.

Data source description

Indoor experiment, self generated.

Data processing method

The O3 oxidation experiment operates in an intermittent manner. Firstly, wash the reactor with deionized water, inject the prepared simulated beneficiation wastewater into the reactor at one time through the peristaltic pump, turn on the ozonator, and after the ozonator is preheated and the generation of O3 is stable, start to pass the ozone gas into the air distribution plate at the bottom of the reactor, Control the gas flow meter to keep the flow rate of O3 gas at 100 ml / min. adjust the power knob of the ozone generator to control the dosage of O3 at 1 ~ 10 mg / L. take the reaction solution after different reaction times for water quality detection, and obtain the corresponding experimental results.

Data quality description

<p>&emsp;Good data quality.

Base information

collect time:2018/10/01-2018/10/31

collect place:Beijing

data size:5.3 MiB

data format:

Coordinate system: 无

Keywords

Theme:Flotation wastewater, ozone oxidation, CODcr
	Subject:geology 
	Time:2018
	Place:Beijing

Space scope

|  | north： 41.60 |  |
| --- | --- | --- |
| west：117.40 |  | east：115.70 |
|  | south： 39.37 |  |

Service information

contacts:Min Yufang

phone:0931-4967596

mailbox:ncdc@lzb.ac.cn

Contact information

contributors:

author:

manager:MIN Yufang

Project information

number:2018YFC0406400，
      name:

Citations and annotations

In order to protect the rights and interests of the platform's scientific and technological resources, expand the services of the platform center, and enhance the application potential of scientific and technological resources,resource users are requested to mark and quote the research results (including published papers, treatises, data products, unpublished research reports, data products, etc.) generated by the use of resources in the following manner.

For the achievements published in English, please refer to the following specifications：

The dataset is provided by National Cryosphere Desert Data Center(https://www.ncdc.ac.cn).

Data reference:

. Research data set on mineral processing wastewater treatment of tungsten molybdenum ore containing salt hydroxamic acid (October 2018). National Cryosphere Desert Data Center(http://www.ncdc.ac.cn), 2022. https://cstr.cn/CSTR:11738.11.ncdc.UTCMW.db2148.2022.