Data set of optimal conditions for acid mine water effluent from high efficiency magnetic separation device experiment (may 2021)

DOI：10.12072/ncdc.UTCMW.db2124.2022

CSTR：11738.11.ncdc.UTCMW.db2124.2022

Share type:Apply to Access

Category:Others

Datasets description

Taking the laboratory water distribution as the research object, the magnetic separation device is used to explore the optimal experimental conditions to ensure that the final effluent turbidity meets the requirements. The optimized experimental factors include pulverized coal particle size ratio, PAC dosage, PAM dosage, PAM type, magnetic particle dosage, magnetic particle type, magnetic particle size, SS initial concentration, drum speed, water inflow, etc. The data set contains 163 data.

Data source description

Indoor experiment, self generated.

Data processing method

Place the prepared simulated wastewater in the raw water tank, turn on the peristaltic pump to pump the raw water, PAC and magnetic powder into the magnetic flocculation tank, and stir it quickly at 160 R / min for 5 min, then turn on the valve of the magnetic flocculation tank to feed water into the reaction tank, add PAM, stir it slowly at 80 R / min for 3 min, and then enter the super magnetic separator through the spring flowmeter to separate the magnetic floc from water, and then the magnetic floc enters the high-speed shear and is sheared into magnetic powder and pulverized coal, Finally, the magnetic powder enters the super magnetic recovery machine for recovery. Take out the outlet water, measure its turbidity and calculate the removal rate, screen out the optimal coagulant, coagulant aid, magnetic powder and the optimal dosage, further change the influencing factors such as the initial concentration of SS, drum speed, pulverized coal particle size and inlet flow, determine the optimal hydraulic conditions for magnetic separation treatment of simulated high turbidity mine water wastewater, and finally determine the recovery rate of magnetic powder under the optimal conditions.

Data quality description

<p>&emsp;Good data quality.

Base information

collect time:2021/05/01-2021/05/31

collect place:Beijing

data size:10.0 MiB

data format:

Coordinate system: 无

Keywords

Theme:Mine water treatment, high efficiency magnetic separation device, turbidity
	Subject:
	Time:2021
	Place:Beijing

Space scope

|  | north： 41.60 |  |
| --- | --- | --- |
| west：117.40 |  | east：115.70 |
|  | south： 39.38 |  |

Service information

contacts:Min Yufang

phone:0931-4967596

mailbox:ncdc@lzb.ac.cn

Contact information

contributors:

author:

manager:MIN Yufang

Project information

number:2018YFC0406400，
      name:

Citations and annotations

In order to protect the rights and interests of the platform's scientific and technological resources, expand the services of the platform center, and enhance the application potential of scientific and technological resources,resource users are requested to mark and quote the research results (including published papers, treatises, data products, unpublished research reports, data products, etc.) generated by the use of resources in the following manner.

For the achievements published in English, please refer to the following specifications：

The dataset is provided by National Cryosphere Desert Data Center(https://www.ncdc.ac.cn).

Data reference:

. Data set of optimal conditions for acid mine water effluent from high efficiency magnetic separation device experiment (may 2021). National Cryosphere Desert Data Center(http://www.ncdc.ac.cn), 2022. https://cstr.cn/CSTR:11738.11.ncdc.UTCMW.db2124.2022.